## Slide 1
OF EXPERIMENTAL STATION
HEFEILIGHT SOURCE INTRODUCTION
合
肥
光
源
HEFEI
LIGHT SOURCE
XMCD Beamline

## Slide 2
01
02
03
04
Introduction
Scientific cases
Methods
Beamtime application
目录
CATALOG

## Slide 3
Beamline Layout
——两分支线+三站
BL12B-b分线
XAS spectra
In-situ XAS
BL12B-a分线
Vector-XMCD
beamline | Beam energy(eV) | resolution(E/⊿E) | Flux | beamsize
BL12B-a | 100-1000 | 2400@244eV | 2x109 phs/s @244eV | 1x0.5mm2
BL12B-b | 50-1000 | 2300@244eV | 1.8x1010 phs/s @244eV | 1x0.5mm2
线站在环厅③号门位置
BL12B-b分线
BL12B-a分线

## Slide 4
Beamline Layout
Vector Magnet Station
Mode：TEY、Transmission
Chamber：XAS，XMCD, XMLD
Temperature：10K-300K
Magnetic Field：0-0.8T
Sample holder
Vertor-magnet

## Slide 5
Beamline Layout
Mode：TEY/TFY/PFY/XEOL
Chamber： XAS，XEOL
Temperature：90K-300K
Sample transfer：in-situ
Transfer
XAS station

## Slide 6
Beamline Layout
Mode：TEY/PFY
Sample holder
In-situ XAS
In-situ Dynamic Liquid-phase Reaction Cell
In-situ Dynamic Liquid-phase Reaction Cell
In-situ Dynamic Liquid-phase Reaction Cell

## Slide 7
01
02
03
04
目录
CATALOG
Introduction
Scientific cases
Methods
Beamtime application

## Slide 8
Experimental Method: X-ray Absorption Spectroscopy(XAS)
1s
2s
2p
Incidence:
Tunable photon
1s
2s
2p
Detection:
Emitted electron
1s
2s
2p
Detection:
Emitted photon
Electron Yield
Signal：Auger electrons, photoelectrons, and secondary electrons
Detection Depth：1 ~ 8 nm
Fluorescence Yield
Signal ：Fluorescent Photons
Detection Depth：100 nm ~ several um
X-rays
photon
Advantage: Element-specific resolution, enabling probing of the local atomic structure and electronic structure of absorbing atoms.

## Slide 9
Experimental Method: X-ray Magnetic Circular Dichroism
Electron Yield
Signal：Auger electrons, photoelectrons, and secondary electrons
Detection Depth：1 ~ 8 nm
Transimission Mode
Luminiscence yield Mode
Advantages:
​1: Quantitative separation of electron spin magnetic moment and orbital magnetic moment​
​2: Element-specific resolution​ (distinctly identifies contributions of different elements to macroscopic magnetism)
​3: High surface sensitivity​ (electron yield mode)
Spin and orbital moment: XMCD theory
轨道占据
自旋磁矩
轨道磁矩

## Slide 10
Experimental Method: X-ray Magnetic Linear Dichroism
Advantages:
​Enables measurement of crystal field effects via X-ray Linear Dichroism (XLD)​​
​Determines antiferromagnetic spin orientation using XMLD – one of the few direct methods for probing antiferromagnetic information​
​High surface sensitivity (electron yield mode)​
XMLD theory
Electron Yield
Signal：Auger electrons, photoelectrons, and secondary electrons
Detection Depth：1 ~ 8 nm
Transimission Mode
Luminiscence yield Mode

## Slide 11
01
02
03
04
目录
CATALOG
Introduction
Scientific cases
Methods
Beamtime application

## Slide 12
Absorption spectroscopy is an effective tool for probing microscopic structures
Science 2020, 370, 192-197
Soft X-ray absorption spectroscopy probes the C K-edge and P L-edge in battery materials, revealing atomic coordination environments and electronic structures. It elucidates energy storage mechanisms, providing a powerful foundational tool for advancing from material observation science to material control science.

## Slide 13
Absorption Spectroscopy Deciphers Coordination Environments and Electronic Structures
Nature Nanotechnol. 2020, 16, 325-330
Soft X-ray absorption spectroscopy probes the N K-edge in energy catalytic materials, resolving atomic coordination environments and electronic structures. Integrated with complementary characterization data, it elucidates catalytic reaction mechanisms.

## Slide 14
XMCD Technique Probes Magnetic Properties
XMCD plays a pivotal role in 2D magnetic materials research, enabling the detection of: Magnetic strength variation across ferromagnetic layers; Saturation field magnitudes; Easy magnetization axes; Orbital magnetic moments; Spin magnetic moments。
Sci. Adv. 6, eabb5157 (2020)

## Slide 15
Utilizing interfacial coupling between ferromagnetic (FM) and antiferromagnetic (AFM) layers, the application of a magnetic field rotates the FM layer's magnetic moment, thereby engineering single-domain or spring-type domain wall configurations within the AFM layer
PRB 91,104424 (2015); Phys. Rev. Mater. 3,114415 (2019)
XMLD Technique Probes Antiferromagnetic Spin Orientation

## Slide 16
X-ray Absorption Spectroscopy (XAS) plays a critical role in analyzing element valence states in ferroelectric materials, while X-ray Linear Dichroism (XLD) effectively determines crystal field variations and probes lattice distortions.
ACS Appl. Mater. Interfaces 12, 43257 (2020)
Combined XAS and XLD Spectroscopy for Resolving Crystal Field Effects

## Slide 17
Combined XAS, XMCD, and XLD Techniques for Superlattice Characterization
The combined application of XAS, XMCD, and XLD techniques provides comprehensive characterization of superlattice samples, resolving: Elemental valence states and charge transfer; Magnetic strength and ferromagnetic-antiferromagnetic phase transitions; Crystal field distortions .
Q. Jin et al., PRL 128, 017202 (2022)

## Slide 18
01
02
03
04
目录
CATALOG
Introduction
Scientific cases
Methods
Beamtime application

## Slide 19
Registration @ https：//lssf.cas.cn
Proposal Submission
Proposal Review
Beamtime Application & Usage, Detailed procedures: http://www.nsrl.ustc.edu.cn/2016/0425/c10980a124134/page.htm
Follow updates via：
User Guide for NSRL (Hefei Light Source) Facility Access

## Slide 20
Contact
Yan Wensheng
0551-63602131
ywsh2000@ustc.edu.cn
Zhang Wenhua
0551-63601992
zhangwh@ustc.edu.cn
Chen Kai
18214752842
kaichen2021@ustc.edu.cn

## Slide 21
Contact
Wang Chao
0551-63602060
chaowng@ustc.edu.cn
Chen Shuangming
0551-63607731
csmp@ustc.edu.cn
Hu Fengchun
0551-63602060 fchu@ustc.edu.cn
Li Qian
0551-63607465 liqian89@ustc.edu.cn

## Slide 22
红外谱学和显微成像光束线站：
联系人：戚泽明
E-mail：zmqi@ustc.edu.cn
原子分子物理光束线站
联系人：王占东
E-mail：zhdwang@ustc.edu.cn
燃烧光束线站
联系人：杨玖重
E-mail：jzyang@ustc.edu.cn
光电子能谱光束线站
联系人：潘海斌
E-mail：hbpan@ustc.edu.cn
质谱光束线站
联系人：潘 洋
E-mail：panyang@ustc.edu.cn
催化与表面科学光束线站
联系人：朱俊发
E-mail：jfzhu@ustc.edu.cn
软X射线成像光束线站
联系人：刘 刚
E-mail：liugang@ustc.edu.cn
软X射线磁性圆二色（XMCD）光束线站
联系人：闫文盛
E-mail：ywsh2000@ustc.edu.cn
角分辨光电子能谱（ARPES）光束线站
联系人：孙 喆
E-mail：zsun@ustc.edu.cn
光谱辐射标准和计量光束线站
联系人：周洪军
E-mail：hjzhou@ustc.edu.cn
用户办联系人： 江 芳
电 话：0551-63602018（24h）
E-mail：jiangf@ustc.edu.cn
保卫室：0551-63602020
辐射防护紧急联系：0551-63602026
西区专家楼订房电话：0551-63602880
联系我们

## Slide 23
谢谢
中国科技大学
国家同步辐射实验室